z2
User name: Phenom-Workstation\Phenom
Phenom User Interface version: 2.0.1-rel
Contains 1 image(s) with a total of 1 analyses

01. Image 1

1 analyses: 1x map

Image 1
1. Map
Complete map

FW: 68 μm, Mode: 15 kV - Image, WD: 8.0 mm, Detector: SED, Time: 4/22/25 3:15 PM
Element Number	Element Symbol	Element Name	Atomic Conc. [%]	Weight Conc. [%]
6	C	Carbon	35.42	20.90
7	N	Nitrogen	1.75	1.21
8	O	Oxygen	30.30	23.82
11	Na	Sodium	14.76	16.68
14	Si	Silicon	3.93	5.43
17	Cl	Chlorine	8.25	14.37
28	Ni	Nickel	4.91	14.17
45	Rh	Rhodium	0.68	3.42

60 625 counts in 0:02:21 (427 c/s)

Disabled elements: -
Cut out of map (resolution: 240×151 points)

Carbon	Nitrogen

Oxygen	Sodium

Silicon	Chlorine

Nickel	Rhodium